Table of Contents

[1 Chapter 1 – Introduction and Overview of X-ray Spectroscopy 1](#_Toc116991460)

[1.1 X-ray absorption spectroscopy 1](#_Toc116991461)

[1.1.1 Experimental modes 2](#_Toc116991462)

[1.2 M- K- and L- Edges 3](#_Toc116991463)

[1.2.1 Experimental considerations 4](#_Toc116991464)

[1.2.2 Regions of XAS spectra 5](#_Toc116991465)

[1.2.3 XANES 6](#_Toc116991466)

[1.2.3.1 XANES processing 6](#_Toc116991467)

[1.2.4 EXAFS 7](#_Toc116991468)

[1.2.4.1 EXAFS processing 7](#_Toc116991469)

[1.3 X-ray emission spectroscopy 7](#_Toc116991470)

[1.3.1 CTC-XES 8](#_Toc116991471)

[1.3.2 VtC-XES 9](#_Toc116991472)

[1.4 Are XANES and VtC-XES complimentary 9](#_Toc116991473)

[1.5 References 9](#_Toc116991474)

# Chapter 1 – Introduction and Overview of X-ray Spectroscopy

The following chapter gives a brief overview of X-ray absorption and emission spectroscopies, including nomenclature and typical uses. For a more detailed discussion, see Rehr and Albers [Rehr, 2000 #95], Sayers, Stern, and Lytle [Sayers, 1971 #241], Bunker [Bunker, #92], Ashley and Doniach [Ashley, 1975], and Glatzel and Bergmann [Glatzel, #58].

## X-ray absorption spectroscopy

X-ray absorption spectroscopy (XAS) has been used as an important tool in many fields of science, such as materials science, physics, biology, chemistry, geosciences, and electronics. XAS is a bulk probe of both electronic and geometric structure around a chosen atomic species and is sensitive to properties such as oxidation state, valency, coordination, and bond length. When X-rays are shone onto a sample, they can either kick the electron out of the system (for X-ray Photoelectron Spectroscopy, or XPS) or push the system into an excited stated by kicking the electron to an unoccupied energy level (for XAS). There is an intrinsic lifetime of this excited state unique to the atomic species and hole. Finally, an electron from an occupied state will fall back down to fill the hole (creating X-ray emission spectroscopy, or XES) or radiate via two-electron processes, such as through the Auger−Meitner effect, as demonstrated in Fig. 1.




Fig. 1 The Auger-Meitner effect is a two-electron process, where an inner-shell electron falls to fill the core hole, thus emitting a photon, but the rest of the extra energy is dissipated by emitting a valence electron.

### Experimental modes

Experimentally, XAS can be either in transmission or florescence mode. Transmission mode is when the monochromatized X-rays must pass through the sample before entering the detector. Florescence mode occurs when the monochromatized X-rays hit the sample and the fluorescence off the sample enter the detector. In florescence mode, there is no background shape (besides stray scatter, if there is any). Fluorescence mode is different from X-ray emission spectroscopy due to the placement of the monochromator; in XES, the sample fluorescence passes to a monochromator, whereas in florescence mode of XAS, the already monochromatized X-rays hit the samples, which then fluoresces.

When in transmission mode, the shape of the background is important to identify the XAS spectra, given by the absorption coefficient µ(E). Transmission-mode XAS is governed by the equation I = I0e-µx, where x is the sample thickness, I is the loss spectra (i.e., the photon counts after passing through the sample) and I0 is the X-ray spectrum without sample. A cross-section is shown in Fig. 2. [Rehr, 2000 #95] We could trivially solve for µ(E) as – ln (I / I0).




Fig. 2 Absorption coefficient for XAS. Taken from Rehr and Albers. [Rehr, 2000 #95]

## M- K- and L- Edges

µ(E) looks like a set of stairs, where each step, or edge, corresponds to an excitation energy of different inner-shell electrons. Each edge has a name and are commonly referred to using the IUPAC notation, as shown in Fig. 3. Exciting electrons from the 1s (n = 1) shell is called K-edge spectroscopy, while exciting electrons from the n = 2 shell are the L edges and the n = 3 the M edges. Each edge is then broken down further based the orbital angular momentum quantum number (l) and the magnetic quantum number (j). For example, exciting the 2s shell is the L1 edge, exciting from the 2p1/2 shell is the L2 edge, and from the 2p3/2 shell is the L3 edge. The same pattern continues for the M edges.

A picture containing text

Description automatically generated

Fig. 3 Absorption edge of an element can be broken down into K, L, and M edges.

### Experimental considerations

Because X-ray absorption spectroscopy is dominated by photoelectric effect, and thus the strongest contributions are from dipole-allowed transitions, choosing which edge to probe depends both on the quantum numbers of the valence shell of a chosen element (i.e., the target electronic states) as well as experimental capabilities (such as energy ranges that can be achieved by the beam, photon counts, and any contamination from the characteristic fluorescence lines from the X-ray source).

Moreover, the ideal sample thickness is one that gives an edge step of approximately 2 [cite]. This ideal absorption is due to the Poisson statistics of the photon counts, and the ratio of the noise to both the background and EXAFS oscillations.

### Regions of XAS spectra




Fig. 4 The XANES and EXAFS regions of XAS spectra.

Zooming in onto these edges, you will see characteristic oscillations. The XAS spectrum can be broken into two different regions – X-ray absorption near edge fine structure (XANES) and Extended X-ray Absorption Fine Structure (EXAFS). [Rehr, 2000 #95] XANES includes any pre-edge features, shoulders, and the region around the edge step, while the EXAFS includes the oscillations at higher energy.

#### XANES

X-ray absorption near edge fine structure (XANES) is the region of XAS around the absorption edge, from any pre-edge features to about 50 eV past the edge, depending on the system. Because XANES probes electronic states near the Fermi level, it is sensitive to local electronic structure around the chosen atomic species, such as oxidation, spin, and valency. Calculating XANES spectra requires full multiple scattering theory and has broadening to transitions due to the lifetime of the core hole.

##### XANES processing

Because spectral features in the XANES spectra are often correlated, meaning two chemical properties can cause the same spectral trends, the most common analysis for XANES spectra is linear combination fitting onto reference spectra. Selecting reference spectra can be tricky because they must encapsulate the experimental domain, so they rely on prior knowledge of the scientific system. Moreover, differences in the second and third coordination shells between the reference structures and experimental sample can have negative influences on the reliability of these fits. [Jahrman, 2022]

Furthermore, proper fitting requires proper “normalization,” as defined by the standard processing tools in Athena [Ravel, 2005] and Larch [Newville, 2013]. Normalizing XANES spectra is defined as fitting a pre-edge line and a post-edge polynomial function (either constant, linear, or quadratic), where the edge is determined as the maximum of the derivative. The pre-edge fit is then subtracted from the entire XANES spectrum, and the post-edge is rescaled such that the fitted polynomial curve falls along the line y = 1 after the edge. This process not only removes global scaling due to differences in sample thickness (i.e., number of atoms), but gives a consistent spectral shape.

#### EXAFS

Extended X-ray Absorption Fine Structure (EXAFS) is weak multiple scattering and the higher energy oscillations past the absorption edge. EXAFS is sensitive to local geometric structure, such as coordination and bond length. Calculating EXAFS involves multiple scattering and the assumption of a muffin-tin potential, and much work has been done to utilize real-space Green’s functions to quickly calculate EXFAS via the FEFF program. [Rehr, 2010]

##### EXAFS processing

An important aspect of EXAFS analysis derives from the parameters in the EXAFS equation. (Go into the EXAFS equation and Fourier transforms)

This analysis is done using the community standard tools: Athena [Ravel, 2005] and its newer cousin Larch [Newville, 2013].

##### Wavelets

Another qualitative analysis of EXAFS that has seen recent traction is wavelet analysis.




Fig. 5 Wavelet analysis

## X-ray emission spectroscopy

X-ray emission spectroscopy (XES) occurs when an excited atom emits a photon as an electron falls to fill the vacancy. Emission lines are similarly named as XAS by the hole location, or shell in which the electron was originally excited from. For example, having electrons fall into a 1s core hole is K fluorescence. The initial shell of the falling electron then dictates whether the spectra are Kα (2p to 1s) or Kβ (3p to 1s). A breakdown of the




Fig. 6 Conventional naming of florescence lines.

The relative intensity of the different K emission lines is demonstrated in Fig. 7. Here, the Kα lines are much more intense (by a factor of about 3) than the Kβ lines. Furthermore, the Kβ satellite lines (or electrons falling from the valence shell) are smaller by a factor of about 500. This difference in photon counts is exactly due to dipole selection rules and is important to consider when deciding on which emission line to probe.




Fig. 7 The Mn K-fluorescence lines for MnO. [Glatzel, #58]

### CtC-XES

Core-to-core X-ray emission spectroscopy (CtC-XES) includes the Kα and Kβ lines (at least for 3d transitions metals) as the valence shell. An in-depth discussion of CtC-XES is included in Glatzel and Bergmann. [Glatzel, #58] The utility of XES was notably demonstrated in Bergmann, et al. [Bergmann, 1998], which studied the oxidation state of Mn in Photosystem II via the Kβ emission lines.

One benefit of Kα emission spectra is that it is not sensitive to environmental factors as the orbitals are too deep to be drastically hybridized. Thus, it has been shown that the integral of the Kα spectra is directly proportional to the number of atoms. Thus, the integral of the Kα spectra can be used as a normalization scaling factor for the other K emission lines.

### VtC-XES

The Kβ satellite lines are also called Valence to Core XES (VtC-XES). Study of the VtC-XES has been relatively new because only the recent improvements in synchrotron and lab-based spectrometers has made this experiment possible. Notably, Pollock and coworkers have developed a theoretical approach to calculating VtC-XES [Pollock, 2014] and used it to study the iron oxidation in the iron-molybdenum cofactor (FeMoco) in nitrogenase. [Lancaster, 2011] However, although VtC-XES is sensitive to ligand identity and other ligand properties, it is not a good quantitative method (rather, it qualitatively follows trends) to determining those properties. [Pollock, 2015] Finally, Holden, et al. [Holden, 2019] studied the exact sensitivity in

## Are XANES and VtC-XES complimentary

XANES and VtC-XES are often seen as complimentary [cite].

* Is this a good section? Find more cites.




Fig. 8 XANES versus VtC-XES

## References